# LOCK-N-STITCH Inc.

# Casting Repair Specialists

# 1015 S. Soderquist Rd.

# Turlock CA 95380

# Final Report

Customer:  L&H Industrial	Phone:  	(480) 968-6141

Contact: 	Wayne Myers				Alt phone: (602) 321-9597 (cell)

Address: 	1710 W. Broadway Road	Fax: 	(480) 894-2644

Tempe, AZ  85282	Date: 	12/13/2012

Part: 10 x 10 Discharge Head Mfg. Marcy

Serial number: #18				    	Inspected by: Jeff Reed

13.  Inspection method(s)

Mag Particle check.

_______________________________________________________________________

_______________________________________________________________________

14.  Damage found:

1 crack found on multiple surfaces. Below are the measurements of each surface and photos.

1A and 1B

Crack starts at 1A, measuring 4.5” long. It proceeds onto surface 1B, and measures 2.75” long. 1A is in rough casting, while 1B is a machined surface.

Metal stitched 1A: 4.5” long by 2” deep, using C4B stitching pins and 2” long by 1” deep using C3B stitching pins.

Metal stitched 1B 2.75” long by 0.5” deep, using C2.5A pins.

Installed (1) L60S lock and (3) L60B bottom locks in 1A. (Retained locks with (2) L6A pins).

Completed crack repair for 1A and 1B:

1C

This is the top flange with thru-hole bolt holes. The crack runs through the flange completely. Measurements of the flange are 5.125” x 2.5” thick. Crack measures 3.75” from the hole shown.

Metal stitched 1C, 5.125” long by 2.5” deep, using C4C stitching pins; and 2.5” long by 0.5” deep using C2.5A stitching pins, on outside of outer bolt hole flange.

Installed (1) L60S lock, (4) L60B locks, (1) L40S lock and (4) L40B locks in 1C. (Retained locks with (4) L6A pins).

Completed crack repair for 1C:

1D

Crack is 5” long before it runs into lower flange. Crack is 3” from hole shown in this photo.

Metal stitched 1D, 5.0” long by 2” deep, using C4B stitching pins.

Installed (2) surface L40S locks and (6) L40B bottom locks in 1D. (Retained locks with (2) L6A pins).

Metal stitch corners on 1D, 1.5” long by 1” deep, using C3B stitching pins.

Completed crack repair for 1D:

1E

The crack then runs through the thru-hole bolt hole. The bolt hole measures is 1.620 x 2.75 deep. The lower flange is 3.75” x 2.75” thick.

Metal stitched 1E using (1) C4C stitching pin and (1) C3C stitching pin.

Completed crack repair for 1E:

(Please note: arrow is pointing to 1E)

1F

Shows the thickness of the lower flange (2.75” thick)

Metal stitched 1F crack, 2.75” long by 0.5” deep, using C2.5A stitching pins.

Completed crack repair for 1F:

1G

This is the surface on the bottom, next to the lower flange. It measures 2.75”.

Metal stitched 1G crack, 2.75” long by 3” deep, using C4C stitching pins.

Installed (1) L50S lock and (5) L50B bottom locks in 1G. (Retained lock with (2) L6A pins).

Completed crack repair for 1G:

1H

This is the back side to 1D (or inside the Discharge Head). It measures 4.5”.

Metal stitched 1H crack, 4.5” long by 3” deep.

Installed (1) L60S lock and (2) L60B bottom locks in 1H. (Retained locks with (2) L6A pins).

1J

Measures 3.75” before it turns up behind the liner. They are removing the liner for more measurements.

Metal stitch 1J crack, 9” long by 1” deep.

Completed crack repair for 1H and 1J:

Conclusion:

Warranty available:

This limited warranty covers our materials and workmanship for the repair of your part. Disassembly and downtime are not covered by this warranty. The limited warranty is for a period of one year from the date of completion of the repair. If there should be any failure in our repair during that period of time due to faulty materials and or workmanship, we will again repair the part at our cost including all labor, materials and travel expense, or we could choose to refund the money you paid for the repair in part or full. We reserve the right to make the final decision whether to repair or refund. This is the limit of our liability. Be aware that we are not responsible for failures due to faulty installation or improper operation and maintenance of the part. If the problem that caused the original damage has not been remedied this warranty will become null and void.

Extended warranty:

# Text boxes

# 800-736-8261

# 209 632-2345

# Fax 209-632-1740

# www.locknstitch.com

4.  Cause of damage

 impact

 heat

 freezing

( normal operation

 other ____________________

5.  Length of crack/s

1A  4.5”		1F  2.75”

1B  2.75”		1G  5.75”

1C  5.125”		1H  4.5”

1D  5”			1J  3.75”

1E  3.75”		1K  ?

6.  Material thickness: 2.5” -- 2.75”

7.  Operating pressure: Static

1.  Base metal

( cast iron

 ductile iron

 cast steel

 cast aluminum

 other ____________________

2.  Machinability

( no previous repairs

 arc-welded

 brazed

 heat-related cracks

 other ____________________

3.  Casting shape where cracked

( flat

( inside/outside corner

( radius

 other ____________________

8.  Operating temperature:

Under 100 degrees

9.  Working environment

 hot

 cold

 safety concerns

describe: ________________

________________________

___________________________

 other ____________________

10.  Remachining requirements

( bolt holes

 bearing bores

( machined surfaces

( Grind to blend

11.  Customer’s needs

( permanent repair

 temporary repair

( turnaround time

Describe: Start as soon as Sunday, November 25, 2012

 other ____________________

12.  Accessibility

( room for the tools?

( room for the operator/s?

( need for disassembly?

Describe: Customer to remove liners and sandblast prior to LNS starting.

 other ____________________