## Slide 1
Deepwater Pathfinder
Repair completed by LOCK-N-STITCH Inc.
September 2012

## Slide 2
Water jacket to air box crack completed

## Slide 3
Lower bore repair side A2 needs two more pins and finish work

## Slide 4
Bores A2 and B2 are bored and ready to accept repair sleeves

## Slide 5
Using liquid Nitrogen to shrink the repair sleeve for the lower bores

## Slide 6
Lower bore repair sleeve installed and ready for final machining

## Slide 7
Stiffening bracket side A2 completed

## Slide 8
Stiffening bracket side B2 is stitched and ready for finish work

## Slide 9
Side B2 main bearing web damage removed and ready to be stitched

## Slide 10
B Side Main Bearing Wall damage casting metal stitching completed and ready to be hand finished

## Slide 11
Inspection door side A2 damaged cut out and ready for new casting

## Slide 12
A Side Inspection gasket surface stitched into place

## Slide 13
A side inspection door gasket surface repaired and machined

## Slide 14
Inspection door B2 damage cut out and still need to cut damaged pocket above door

## Slide 15
B side inspection gasket surface casting fitted and ready to be metal stitched

## Slide 16
Metal stitching in process on the B side Inspection Door Gasket Surface

## Slide 17
B Side Inspection Door gasket Surface

## Slide 18
7’ Climax bed Mill machining the gasket surfaces on the inspection door

## Slide 20
1. LNS technicians performed in‐process and final inspections of each
repair site once the metal stitching process for that area was
concluded.
2. The process involved using a magnetic particle inspection process
with either dry powder or wet particle methods.
3. The metal stitching locks and stitching pins have magnetic properties
that are slightly different from the cast iron so the outline of the
repairs attracts the magnetic powder when a special magnet is
placed on the part with the North and south poles spanning the
repair.
4. This method quickly and easily shows any gaps between the pins or
any crack that may have been missed.
5. If a gap is detected on either side of the repaired wall, additional
stitching pins could have been added to the repair.
6. The final inspection showed no spaces, gaps or cracks at or around
the metal stitching repairs that were repaired.
Final repair inspection process

## Slide 21
This repair required eight (8) weeks to complete and is guaranteed for one year.